| Parameter | FeS2 (Absorber Layer) | Scientific Basis | SnS2 :Co (Buffer Layer) | Scientific Basis |
| --- | --- | --- | --- | --- |
| Eg (eV) | 1.6 | Matches the experimental Pyrite FeS2 gap (40 min.). | 2.25 | Matches our previous experimental results. |
| Thickness (µm) | 1.5 | Matches the experimental thickest film (~1.53 µm). | 0.05 | Standard thickness in heterojunction devices |
| χ (Electron affinity) (eV) | 4.5 | Typical electron affinity values used for FeS2 heterojunction modeling. | 4.20 | Needed for FeS2/SnS2 conduction band offset |
| εr (Relative permittivity) | 10.9 | Reported dielectric constant of pyrite. | 8.5 | Reported for hexagonal SnS2 |
| Nc (cm-3) | 2.2 × 1018 | Effective DOS in conduction band (SCAPS standard semiconductor approximation). | 2.2 × 1018 | SCAPS default for wide-gap semiconductors |
| Nv (cm-3) | 1.8 × 1019 | Effective DOS in valence band. | 1.8 × 1019 | Standard approximation |
| μe (cm2 V-1 s-1) | 80 | Electron mobility values reported for pyrite single-phase films. | 30 | Reported for SnS2 nanosheets and thin films |
| μh (cm2 V-1 s-1) | 20 | Hole mobility is lower due to stronger scattering. | 5 | Lower due to layered transport anisotropy |
| ND (cm-3) | 1 × 1016 | Typical donor density for slightly n-type pyrite films. | 1018 | Co doping enhances n-type conductivity |
| NA (cm-3) | 0 | Usually negligible unless intentionally p-doped. | 0 | SnS2 remains strongly n-type |
| Electron/Hole Thermal velocity (cm/s) | 1 × 107 | Standard SCAPS default for carriers. | 1 × 10⁷ | Standard semiconductor assumption |

Table S2. Electronic and optical parameters used for the FeS2 absorber layer in SCAPS-1D simulations, collected from experimental reports and standard semiconductor modeling references.

where: Eg: band gap; χ: electron affinity; εr: dielectric permittivity; N: effective band states density (for the conduction band C and the valence band V); μ: charge carrier mobility (for e: electrons and h: holes); N: defect density (for donors D and acceptors A).