Supplementary information

Machine Learning for Density Prediction and Process Development of Large Layer Thickness LPBF 304L Stainless Steel and Its Mechanical Impacts

- Data preprocessing and volumetric energy density

The dataset contains four process variables—layer thickness 𝐻 (μm), laser power 𝑃 (W), scan speed 𝑉 (mm/s), and hatch spacing 𝑆 (mm)—and the measured relative density 𝑦 (%). All required columns were converted to numeric values and samples with missing entries were discarded. Non-physical records (𝐻≤0, 𝑃≤0, 𝑉≤0, or 𝑆≤0) were removed. Volumetric energy density was computed as

| E=PVS(H1000) | (1) |
| --- | --- |

where 𝐻/1000 converts thickness from μm to mm. The density target was constrained to physically meaningful bounds. Specifically, if max(𝑦)≤1.5, the target was treated as a ratio and clipped to [0,1]; otherwise the target was treated as percentage and clipped to [0,100]. In this study, the target density is reported in percent and the mechanistic model uses 𝐷max=100%.

To suppress spurious points, a robust outlier filter based on the interquartile range (IQR) was applied to the density target:

| [ymin,ymax]=Q1-3.0⋅IQR,Q3+3.0⋅IQR | （2） |
| --- | --- |

where 𝑄1 and 𝑄3 are the 25th and 75th percentiles, respectively, and 𝐼𝑄𝑅=𝑄3−𝑄1. Samples with y outside this range were removed.

- Stratified splitting strategy

  - Joint strata: thickness × energy bins

To mitigate sampling bias across thickness and energy regimes, all dataset splits were stratified using joint strata defined by the discrete layer thickness and within-thickness energy bins. For each thickness group 𝐻∈{60,90,120}, the computed energy density values 𝐸 were ranked (method = “first”) and discretized into quantile bins using qcut with duplicates="drop". The number of bins per thickness was set to:

- Energy bins per thickness: 𝐾=3

If a thickness group contained insufficient unique 𝐸 values, the effective number of bins was reduced automatically to avoid empty bins. The final stratum label was formatted as:

| stratum=H{H}E{b} | （3） |
| --- | --- |

where 𝑏∈{0,1,2} denotes the energy-bin index within the corresponding thickness group.

  - Outer train–test split (single holdout)

A single holdout split was generated using stratified sampling on the stratum labels:

- Train/test ratio: 80% / 20%

- Stratification: joint stratum labels (thickness × energy-bin)

- Random seed: 42

This outer split was used to report the final test-set performance.

- Feature engineering and preprocessing

  - Engineered features for residual learning

Residual learning uses engineered descriptors that capture heat-input and scan-geometry coupling beyond the explicit mechanistic model. The feature set includes the original process variables, volumetric energy density 𝐸, and additional nonlinear/interaction terms defined in Supplementary Table S1.

Table S1. Input features used by the residual learners.

| Category | Feature name | Definition |
| --- | --- | --- |
| Raw variables | (H) | Layer thickness (μm) |
| Raw variables | (P) | Laser power (W) |
| Raw variables | (V) | Scan speed (mm/s) |
| Raw variables | (S) | Hatch spacing (mm) |
| Energy density | (E) | E=PVS(H1000) |
| Line energy | LED | (P/V) |
| Surface energy proxy | AED | (P/(V S)) |
| Nonlinear transform | logE | log⁡(max(E,10-12)) |
| Inverse-speed | invV | 1/max(V,10-12) |
| Interaction | P_over_S | P/max(S,10-12) |
| Nonlinear energy | E2 | E2 |
| Interaction | E_times_S | E⋅S |
| Interaction | E_over_S | E/max(S,10-12) |
| Interaction | E_over_V | E/max(V,10-12) |
| Categorical thickness | thickness_cat | H cast to string for one-hot encoding |

  - Preprocessing pipeline

A ColumnTransformer was used to preprocess inputs:

- Numeric features: standardized by StandardScaler (zero mean, unit variance)

- Categorical feature: thickness_cat one-hot encoded by OneHotEncoder(handle_unknown="ignore")

The target column (density) and stratum label were excluded from the input matrix.

- Mechanistic model fitting details

  - Mechanistic model form

A thickness-aware dual-mechanism porosity model was adopted:

| Porositymech(E,H)=p0(H)+ALoFe-BLoFE+AkeyσE-Ek(H)sk | (4) |
| --- | --- |

where 𝑝0(𝐻) is a thickness-dependent baseline porosity, the exponential term represents low-energy lack-of-fusion decay, and the sigmoid term represents high-energy instability/keyhole-related growth. The sigmoid is defined as 𝜎(𝑧)=1/(1+exp(−𝑧)). The baseline porosity is constrained to be positive using softplus parameterization:

| p0(H)=log⁡(1+exp⁡(b0(H))) | (5) |
| --- | --- |

The mechanistic density prediction is:

| ymech=Dmax-Porositymech,Dmax=100% | (6) |
| --- | --- |

  - Optimization objective, regularization, and solver settings

Parameters were fitted by minimizing residuals in porosity space using nonlinear least squares with a robust Huber loss:

- Solver: scipy.optimize.least_squares (bounded trust-region reflective)

- Loss: loss="huber"

- Huber scale: f_scale=1.0

- Max function evaluations: max_nfev=5000

A weak regularization was applied to stabilize 𝐸𝑘(𝐻). In implementation, an auxiliary residual term was appended for every training sample:

| rreg=λEk(Hi)-E¯ | (7) |
| --- | --- |

where Eis the mean energy density of the fitted dataset and the regularization strength was:

- λ(EK_REG): 0.002

  - Initialization and parameter bounds

Initialization was:

- ALoF=1.0, BLoF=0.01

- Akey=1.0,Sk=10.0

For each thickness group, Ek(H) initialized to the median of 𝐸 in the fitted set.

For each thickness group, 𝑏0(𝐻) initialized by mapping the median true porosity through inverse-softplus (computed from Porositytrue=𝐷max−𝑦)

Bound constraints were:

- 𝐴LoF∈[0,103],𝐵LoF∈[0,1]

- 𝐴key∈[0,103], 𝑠𝑘∈[10−6,106]

- 𝑏0(𝐻)∈[−20,20]for each thickness group

- 𝐸𝑘(𝐻)∈[0,106]for each thickness group

Predicted mechanistic density was clipped to the same physical bounds used for the target.

  - Reported fitted parameters and parameter identifiability

The fitted parameter values of the two-stage mechanistic model are summarized in Tables S2-S3. Table S2 reports the global parameters controlling the low-energy lack-of-fusion decay term and the high-energy transition term, while Table S3 reports the thickness-specific baseline porosity 𝑝0(𝐻) and transition energy 𝐸𝑘(𝐻). It should be noted that parameter identifiability differs across thickness groups because the experimentally sampled energy-density windows are not equally broad. For the 120 μm group, the sampled range extends sufficiently into the high-energy regime, allowing the transition parameter 𝐸𝑘 to be resolved within the data domain. In contrast, for the 60 μm and 90 μm groups, the fitted 𝐸𝑘 values lie outside or close to the upper boundary of the explored energy-density range. Therefore, for these two groups, the transition parameter should be interpreted as weakly constrained by the available data rather than as a precisely determined physical threshold. Representative mechanistic refit curves for the three thickness groups are shown in Fig. S1.

Table S2. Global fitted parameters of the two-stage mechanistic model.

| Parameter | Value | Interpretation |
| --- | --- | --- |
| ALoF | 0.1755 | Amplitude of the low-energy lack-of-fusion decay term |
| BLoF | 0.00994 | Decay rate of the low-energy lack-of-fusion term |
| Akey | 1.1037 | Amplitude of the high-energy transition term |
| sk​ | 9.1954 | Transition width of the high-energy term |

Table S3. Thickness-specific fitted parameters of the two-stage mechanistic model.

| Layer thickness (μm) | p0​(H) | Ek(H) (J/mm3) | Sampled energy-density range (J/ mm3) |
| --- | --- | --- | --- |
| 60 | 0.0080 | 127.22 | 32.92–72.53 |
| 90 | 0.00003 | 99.66 | 36.06–85.65 |
| 120 | 0.1084 | 91.34 | 40.79–166.46 |

## Fig. S1. Mechanistic refit of porosity as a function of energy density for the 60, 90, and 120 μm layer-thickness groups.

## Symbols denote experimental data and solid curves denote the mechanistic refit within the experimentally sampled energy-density range; dashed curves indicate extrapolation outside the sampled range. Vertical dashed lines mark the fitted transition energy Ek(H). The 120 μm group spans a sufficiently broad high-energy window to resolve the second-stage transition within the sampled domain, whereas the fitted Ek(H) values for the 60 and 90 μm groups lie near or beyond the upper boundary of the sampled range, indicating weaker identifiability of the high-energy transition in these two groups.

- Residual learning, fusion tuning, and evaluation

  - Residual definition and learners

Residual learning was performed in density space. For any training subset:

| ry=y-ymech | (8) |
| --- | --- |

Two residual learners were trained on the engineered features (Table S1):

- Ridge regression for the linear component of 𝑟𝑦

- ExtraTrees regressor for nonlinear structure in 𝑟𝑦

The final fused prediction on any sample is:

| y=clipymech+ωrRidge+(1-ω)rET | (9) |
| --- | --- |

where clipping enforces the same physical bounds as the target.

  - Hyperparameter search space

Inner-loop tuning (performed on the training subset only) selected 𝜔and the Ridge regularization coefficient 𝛼:

- Ridge 𝛼 grid: {10−2,10−1,1,10,100,1000}

- Fusion weight grid: 𝜔∈{0.00,0.05,0.10,…,1.00}

The ExtraTrees residual learner used:

n_estimators=800, max_depth=12, min_samples_leaf=6, min_samples_split=12,

max_features=0.5, bootstrap=True, n_jobs=-1, random_state=42

  - Inner-loop tuning protocol (train only)

Hyperparameters were tuned via repeated stratified cross-validation on the training subset:

- Splitter: RepeatedStratifiedKFold

- Folds: 5

- Repetitions: 10

- Random seed: 42

- Stratification labels: thickness × energy-bin stratum (Section S2.1)

Within each fold:

- Fit the mechanistic model on the fold-training subset; compute ymech

- Compute density residual 𝑟𝑦=𝑦−𝑦mech on the fold-training subset.

- Fit Ridge(𝛼) and ExtraTrees on residuals.

- For each 𝜔 in the grid, predict on the fold-validation subset and compute MAE and 𝑅2.

The selected configuration minimized the mean MAE across the 50 validation runs (5 folds × 10 repeats).

  - Outer-loop evaluation and baseline models

After tuning, the final mechanistic model and residual learners were refit on the full training subset and evaluated on the held-out test subset (Section S2.2). Performance metrics were:

- 𝑅2: coefficient of determination

- MAE: mean absolute error

- RMSE: MSE​

For comparison, two purely data-driven baselines were trained on the same training subset using the same preprocessing pipeline and evaluated on the same test subset:

- RandomForest baseline: n_estimators=800, max_depth=14, min_samples_leaf=4, min_samples_split=10, max_features=0.6, bootstrap=True, n_jobs=-1, random_state=42

- ExtraTrees baseline: n_estimators=800, max_depth=12, min_samples_leaf=6, min_samples_split=12, max_features=0.5, bootstrap=True, n_jobs=-1, random_state=42