Supporting Information

Parametric Design and Characteristic Analysis of Three-Unit-Cell Model in 3D Seven-Directional Braided Compo-sites

Xiyue Zhang1, Feizhou Li1,*, Zhihai Hu1, Weiliang Zhang1, Xindang He4, Gexia Yuan1, Yanwei Feng5, Yafeng Qi2,3,*

1. Institute of Mechanical Engineering, Baoji University of Arts and Sciences, Baoji 721016, China.

2. State Key Laboratory of Electromechanical Integrated Manufacturing of High-performance Electronic Equipment, School of Electro-Mechanical Engineering, Xidian University, Xi’an, Shaanxi 710071, China.

3. State Key Laboratory of Tribology in Advanced Equipment, Tsinghua University, Beijing 100084, China.

4. Department of Mechanics, Civil Engineering and Architecture, Northwestern Polytechnical University, Xi’an 710072, China;

5. College of Electron-mechanics and Automobile Engineering, Tianshui Normal University, Tianshui 741000, China.

This file contains the following contents:

Figure S1-S6

Table S1-S3

Fig. S1 Graphical interface of the parametric design system for 3D seven-directional braided composite

Fig. S2 Yarn numbering: (A) Braiding yarns; (B) Axial yarns, six-directional yarns and seven-directional yarns

Fig. S3 Results of unit-cell mechanical response: (a)~(c) Tension in X, Y, Z directions; (d)~(f) Shear in XY, XZ, YZ directions

Fig. S4. Correlation between  and four characteristic angles (, , , ) at different : (A) =0.3, (B) =0.5

Fig. S5. Effects of  and yarn count on  (A) and  (B)

Fig. S6 Solid models of the internal unit-cells with typical braiding parameters: (A) =45°, =40%, (B) =45°, =30%, (C) =30°, =40%

Table S1 Rotation parameters of yarn instances

| Yarn Number | Length | Rotation Vector |  | Endpoint Coordinates |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Rotation Axis | Rotation Angle | Endpoint 1 | Endpoint 2 |
| 1 | L | (-1,1,0) |  | (1.5W, 0, 0) | (2W, 0.5T, 0.25h) |
| 2 | 3L | (-1,1,0) |  | (0, 0.5T, 0.25h) | (1.5W, 2T, h) |
| 3 | 2L | (-1,1,0) |  | (1.5W, T, 0) | (0.5W, 0, 0.5h) |
| 4 | L | (-1,1,0) |  | (0.5W, 2T, 0.5h) | (0, 1.5T, 0.75h) |
| 5 | L | (-1,1,0) |  | (2W, 1.5T, 0.75h) | (1.5W, T, h) |
| 6 | 3L | (1,1,0) |  | (0.5W, 2T, 0) | (2W, 0.5T, 0.75h) |
| 7 | L | (1,1,0) |  | (0, 0.5T, 0.75h) | (0.5W, 0, h) |
| 8 | L | (1,1,0) |  | (0.5W, T, 0) | (0, 1.5T, 0.25h) |
| 9 | L | (1,1,0) |  | (2W, 1.5T, 0.25h) | (1.5W, 2T, 0.5h) |
| 10 | 2L | (1,1,0) |  | (1.5W, 0, 0.5h) | (0.5W, T, h) |
| 11 | h |  |  | (0, 0, 0) | (0, 0 h) |
| 12 | 2T | (-1,0,0) |  | (0.5W, 0, 0.25h) | (0.5W, 2T, 0.25h) |
| 13 | 2W | (0,1,0) |  | (0, 0.5T, 0) | (2W, 0.5T, 0) |

Table S2 Braiding parameters: symbol and definitions

| Symbol | Definition |
| --- | --- |
|  | Length of the short semi-axis of the woven yarn's elliptical cross-section |
|  | Length of the long semi-axis of the woven yarn's elliptical cross-section |
|  | Horizontal orientation angle |
|  | Internal braiding angle |
|  | Axial yarn cross-sectional dimension coefficient |
|  | Cross-sectional dimension coefficient of six-directional yarns and seven-directional yarns |
|  | Braiding geometric parameter |
|  | Fiber packing factor of braiding yarns |
|  | Fiber packing factor of axial yarns |
|  | Fiber packing factors of six-directional and seven-directional yarns |
|  | Proportional distribution of the three-unit-cells within the composite structure |
|  | Yarn volume fraction of the three-unit-cells |
|  | Yarn volume of the three-unit-cells |
|  | Unit-cell volume of the three-unit-cells |
|  | Yarn volume fraction of the unit-cell |
|  | Fiber packing factor |
|  | Unit-cell volume |
|  | Carbon fiber density |
|  | Matrix density |
|  | Number of rows in yarn carrier array |
|  | Number of columns in yarn carrier array |

Table S3 Comparison table between theoretical values and output parameters of the plugin

| Parameter |  |  | Theoretical Value | Output Value of the Plugin | Error Rate* |
| --- | --- | --- | --- | --- | --- |
| r3=0.18 | =20° | (mm) | 4.155959 | 4.147827 | 0.20% |
|  |  | (%) | 40.00 | 40.17 | 0.43% |
|  |  | (g) | 6.32 | 6.29 | 0.47% |
|  | =30° | (mm) | 2.619979 | 2.614852 | 0.20% |
|  |  | (%) | 40.00 | 40.27 | 0.68% |
|  |  | (g) | 3.99 | 3.97 | 0.50% |
|  | =40° | (mm) | 1.802701 | 1.799173 | 0.20% |
|  |  | (%) | 40.00 | 40.15 | 0.38% |
|  |  | (g) | 2.75 | 2.73 | 0.73% |
|  | =50° | (mm) | 1.269260 | 1.266776 | 0.20% |
|  |  | (%) | 40.00 | 40.28 | 0.70% |
|  |  | (g) | 1.93 | 1.92 | 0.52% |
|  | =60° | (mm) | 0.873326 | 0.871617 | 0.20% |
|  |  | (%) | 40.00 | 40.18 | 0.45% |
|  |  | (g) | 1.33 | 1.32 | 0.76% |
|  | =70° | (mm) | 0.550558 | 0.549481 | 0.20% |
|  |  | (%) | 40.00 | 40.10 | 0.25% |
|  |  | (g) | 0.84 | 0.833 | 0.83% |
| r3=0.31 | =20° | (mm) | 4.443016 | 4.433564 | 0.21% |
|  |  | (%) | 35.00 | 35.18 | 0.51% |
|  |  | (g) | 7.60 | 7.55 | 0.66% |
|  | =30° | (mm) | 2.800943 | 2.794985 | 0.21% |
|  |  | (%) | 35.00 | 35.16 | 0.46% |
|  |  | (g) | 4.79 | 4.76 | 0.63% |
|  | =40° | (mm) | 1.927215 | 1.923115 | 0.21% |
|  |  | (%) | 35.00 | 35.20 | 0.57% |
|  |  | (g) | 3.29 | 3.28 | 0.31% |
|  | =50° | (mm) | 1.356929 | 1.354043 | 0.21% |
|  |  | (%) | 35.00 | 35.23 | 0.66% |
|  |  | (g) | 2.32 | 2.31 | 0.43% |
|  | =60° | (mm) | 0.933648 | 0.931662 | 0.21% |
|  |  | (%) | 35.00 | 35.21 | 0.60% |
|  |  | (g) | 1.60 | 1.59 | 0.63% |
|  | =70° | (mm) | 0.588586 | 0.587333 | 0.21% |
|  |  | (%) | 35.00 | 35.16 | 0.46% |
|  |  | (g) | 1.01 | 1.00 | 0.99% |
| r3=0.48 | =20° | (mm) | 4.798869 | 4.807221 | 0.17% |
|  |  | (%) | 30.00 | 29.89 | 0.37% |
|  |  | (g) | 9.41 | 9.45 | 0.43% |
|  | =30° | (mm) | 3.025279 | 3.030544 | 0.17% |
|  |  | (%) | 30.00 | 29.96 | 0.13% |
|  |  | (g) | 5.93 | 5.96 | 0.51% |
|  | =40° | (mm) | 2.081571 | 2.085194 | 0.17% |
|  |  | (%) | 30.00 | 29.91 | 0.30% |
|  |  | (g) | 4.08 | 4.10 | 0.49% |
|  | =50° | (mm) | 1.465610 | 1.468160 | 0.17% |
|  |  | (%) | 30.00 | 29.87 | 0.43% |
|  |  | (g) | 2.87 | 2.89 | 0.70% |
|  | =60° | (mm) | 1.008426 | 1.010181 | 0.17% |
|  |  | (%) | 30.00 | 29.81 | 0.30% |
|  |  | (g) | 1.98 | 1.99 | 0.51% |
|  | =70° | (mm) | 0.635727 | 0.636833 | 0.17% |
|  |  | (%) | 30.00 | 29.85 | 0.50% |
|  |  | (g) | 1.25 | 1.25 | 0.00% |
| r3=0.68 | =20° | (mm) | 5.256928 | 5.246818 | 0.19% |
|  |  | (%) | 25.00 | 25.08 | 0.32% |
|  |  | (g) | 12.15 | 12.08 | 0.58% |
|  | =30° | (mm) | 3.314046 | 3.307672 | 0.19% |
|  |  | (%) | 25.00 | 25.04 | 0.16% |
|  |  | (g) | 7.66 | 7.62 | 0.52% |
|  | =40° | (mm) | 2.280260 | 2.275874 | 0.19% |
|  |  | (%) | 25.00 | 25.06 | 0.24% |
|  |  | (g) | 5.27 | 5.24 | 0.57% |
|  | =50° | (mm) | 1.605504 | 1.602416 | 0.19% |
|  |  | (%) | 25.00 | 25.10 | 0.40% |
|  |  | (g) | 3.71 | 3.69 | 0.54% |
|  | =60° | (mm) | 1.104682 | 1.102557 | 0.19% |
|  |  | (%) | 25.00 | 25.12 | 0.48% |
|  |  | (g) | 2.55 | 2.54 | 0.39% |
|  | =70° | (mm) | 0.696408 | 0.695069 | 0.19% |
|  |  | (%) | 25.00 | 25.04 | 0.16% |
|  |  | (g) | 1.61 | 1.60 | 0.62% |
| r3=0.97 | =20° | (mm) | 5.877638 | 5.884232 | 0.11% |
|  |  | (%) | 20.00 | 19.94 | 0.30% |
|  |  | (g) | 16.68 | 16.73 | 0.30% |
|  | =30° | (mm) | 3.705351 | 3.709508 | 0.11% |
|  |  | (%) | 20.00 | 19.98 | 0.10% |
|  |  | (g) | 10.51 | 10.55 | 0.38% |
|  | =40° | (mm) | 2.549501 | 2.552361 | 0.11% |
|  |  | (%) | 20.00 | 20.00 | 0.00% |
|  |  | (g) | 7.23 | 7.26 | 0.41% |
|  | =50° | (mm) | 1.795074 | 1.797087 | 0.11% |
|  |  | (%) | 20.00 | 19.95 | 0.25% |
|  |  | (g) | 5.09 | 5.11 | 0.39% |
|  | =60° | (mm) | 1.235117 | 1.236503 | 0.11% |
|  |  | (%) | 20.00 | 19.93 | 0.35% |
|  |  | (g) | 3.50 | 3.52 | 0.57% |
|  | =70° | (mm) | 0.778636 | 0.779510 | 0.11% |
|  |  | (%) | 20.00 | 19.94 | 0.30% |
|  |  | (g) | 2.21 | 2.22 | 0.45% |

*: The error rate = |(Theoretical value - Output value of the plugin) / Theoretical value| × 100%.