Table of content

Figure S1. The structural and compositional analysis of the products with PbI2 assisted growth.

Figure S2. Atomic force microscopy (AFM) characterization of SnS2 nanosheets.

Figure S3. The theoretical calculation of SnS2 crystal properties.

Figure S4. XPS analysis after transferred to SiO2/Si (300 nm SiO2).

Figure S5. The Raman spectroscopy of SnS2 nanosheets on the growth substrate and the transferred substrates.

Supplementary Note 1: The Calculation of Raman Mode Intensity for ARPRS

Supplementary Note 1: The Calculation of Raman Mode Intensity for ARPRS

According to group theory, the Raman tensor for the Raman-active modes of SnS2 on SiO2 can be expressed as[1,2]:

RA1g=a000a000c                           (S1)

The intensity of a Raman active mode with Raman tensor R can be calculated by:

I∝es.R.ei2                                               (S2)

where ei is the incident light polarization unit vector, es is the scattered light unit polarization vector, and R is the Raman tensor of the Raman mode. For parallel polarization configurations, the incident/scattered Raman vector for the polarized light is es= (−sinβ cosβ 0) and ei= (−sinβ cosβ 0)T; for perpendicular polarization configurations, the incident/scattered Raman vector for the polarized light is es= (cosβ sinβ 0) and ei= (−sinβ cosβ 0)T.

For parallel polarization configuration

IA1g//∝es.R.ei2∝-sinβcosβ0a000a000c-sinβcosβ02∝a2        (S3)

For perpendicular polarization configuration

IA1g┴∝es.R.ei2∝cosβsinβ0a000a000c-sinβcosβ02∝0            (S4)

Figure S1. The structural and compositional analysis of the products with PbI2 assisted growth. (a)-(b) SEM image, (c) EDS elemental mapping of Pb, Sn, S and PbSnS3, (d) and (e) XRD pattern and Raman of PbSnS3 nanowire, respectively.

Figure S2. Atomic force microscopy (AFM) characterization of SnS2 nanosheets. (a)-(c) AFM images and corresponding height profiles of SnS2 growth with assistant of the KI, CsCl and KI/CsCl (KI:CsCl=1:1); (d)-(e) the average thickness and length of the SnS2 growth with assistant of the KI, CsCl and KI/CsCl (KI:CsCl=1:1).

Figure S3. The theoretical calculation of SnS2 crystal properties. (a) Formation energy of SnS2 crystal on (100), (010) and (001) plane; (b) Binding energy of Cs and K on SnS2 (100), (010) and (001) surface of SnS2.

Figure S4. XPS analysis after transferred to SiO2/Si (300 nm SiO2). (a) XPS survey spectrum after transferred to SiO2/Si (300 nm SiO2), confirming all expected elements; (b) Sn 3d region, fitted with a single spin-split doublet; (c) S 2p region, deconvoluted into two peaks; (d) Cs 3d region, fitted with a spin-split doublet; (e)-(g) Cl 2p, K 2p, and I 3d regions, showing no detectable signals.

Figure S5. The Raman spectroscopy of SnS2 nanosheets on the growth substrate and the transferred substrates. (a) the Raman spectroscopy of SnS2 nanosheets on the growth substrate and the transferred substrates, including Si, SiO2/Si (300 nm SiO2) and quartz glass; (b) the average Raman peak shift on the growth substrate and the transferred substrates.

Reference

- Loudon, R., The Raman effect in crystals. Adv. Phys. 1964, 13 (52), 423-482.

- Ding, Y.; Zheng, W.; Lu, X.; Liang, Y.; Zhu, Y.; Jin, M.; Huang, F., Raman Tensor of Layered SnS2. The Journal of Physical Chemistry Letters 2020, 11 (23), 10094-10099.