Supplementary Materials

Spontaneous 2D Film Formation of Alkanes on Isoelectronic Substrates: BN Nanosheet vs. Graphene. Quantum Chemical Semi-Empirical Approach

E. S. Kartashynska 1

1 L.M. Litvinenko Institute of Physical Organic and Coal Chemistry, 70 R. Luxemburg Str., 283048, Donetsk, Russian Federation

E-mail: elenafomina-ne@yandex.ru

Table S1. Structural parameters borazole molecule calculated within different methods

| Method | Bond length, Å |  |  | Dipole moment, Debye | Polariz-ability, a.u. |
| --- | --- | --- | --- | --- | --- |
|  | B – N | N – H | B – H |  |  |
| PM6 | 1.4357 | 1.0004 | 1.1939 | 1·10-5 | 51.373 |
| PM6-DH2 | 1.4358 | 1.0003 | 1.1939 | <1·10-5 | 51.378 |
| PM6-D3H4 | 1.4358 | 1.0006 | 1.1943 | <1·10-5 | 51.386 |
| B3LYP-D3/6-311G** (this study) | 1.4290 | 1.009 | 1.192 | 7·10-5 | 55.689 |
| B3LYP / 6-31+G** [1] | 1.4326 | 1.0103 | 1.1947 | 1.049·10-3 | 58.753 |
| CAM-B3LYP / 6-31+G** [1] | 1.4278 | 1.0091 | 1.1945 | 1.217·10-3 | 57.222 |
| B3LYP / 6-311++G** [1] | 1.4308 | 1.0088 | 1.1918 | 7.140·10-4 | 59.787 |
| CAM-B3LYP / 6-311++G** [1] | 1.4279 | 1.0091 | 1.1943 | 1.304·10-3 | 57.503 |
| Exptl. [2, 3] | 1.429-1.431 | - | - | 0 | - |

Table S2. Thermodynamic parameters of formation for alkanes, benzene, borazole, tricircumcoronene and B75N75H30 in gaseous phase within semi-empirical methods

| Molecule | Thermodynamic parameters |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ΔH2980, kJ/mol | S2980, J/(mol·K) | ΔH2980, kJ/mol | S2980, J/(mol·K) | ΔH2980, kJ/mol | S2980, J/(mol·K) | ΔH2980, kJ/mol | S2980, J/(mol·K) |
|  | PM6 |  | PM6-DH2 |  | PM6-D3H4 |  | Experimental values [4] |  |
| CH4 | -51.42 | 186.24 | -51.42 | 186.24 | -7.58 | 186.58 | -74.52 | 186.27 |
| C2H6 | -66.17 | 231.84 | -66.37 | 231.45 | -21.40 | 231.19 | -83.82 | 229.12 |
| C3H16 | -87.73 | 274.63 | -88.65 | 273.12 | -36.13 | 274.12 | -104.68 | 270.20 |
| C4H10 | -108.98 | 308.83 | -110.81 | 306.93 | -50.68 | 308.31 | -125.79 | 309.91 |
| C5H12 | -129.81 | 343.68 | -132.65 | 340.57 | -64.99 | 343.50 | -146.76 | 349.45 |
| C6H14 | -150.77 | 377.52 | -154.64 | 374.42 | -79.44 | 377.26 | -166.94 | 388.74 |
| C7H16 | -171.71 | 412.58 | -176.60 | 406.55 | -93.87 | 412.80 | -187.65 | 427.98 |
| C8H18 | -192.64 | 447.06 | -198.57 | 439.81 | -108.30 | 445.68 | -208.75 | 467.23 |
| C9H20 | -213.58 | 482.74 | -220.55 | 472.90 | -122.74 | 482.59 | -228.74 | 506.40 |
| C10H22 | -234.51 | 516.78 | -242.52 | 506.17 | -137.18 | 516.05 | -249.46 | 545.70 |
| C11H24 | -255.45 | 555.95 | -264.50 | 552.47 | -151.62 | 554.24 | -270.43 | 584.93 |
| C12H26 | -276.38 | 589.90 | -286.47 | 596.17 | -166.06 | 588.93 | -290.72 | 624.15 |
| C13H28 | -297.32 | 631.07 | -308.44 | 631.19 | -180.50 | 623.37 | -311.77 | 663.37 |
| C14H30 | -318.25 | 672.25 | -330.41 | 659.64 | -194.95 | 659.85 | -332.44 | 702.59 |
| C6H6 | 101.22 | 271.44 | 98.23 | 271.32 | 98.73 | 271.45 | 82.60 | 269.20 |
| B3N3H6 | -510.00 | 290.31 | -514.038 | 290.30 | -512.56 | 290.35 | -541.0 (liq.) [5] -519.2±13.4 [6] | 199.6 (liq.) [5] |
| C150H30 | 2048.52 | 1537.29 | 1683.57 | 1476.66 | 1787.16 | 1539.86 | - | - |
| B75N75H30 | -18389.7 | 1964.62 | -18959.3 | 1993.70 | -18640.3 | 1969.96 | - | - |

Table S3. Binding thermodynamic parameters for short-chain alkanes with molecules modelling the surface of BNNS and graphene

| Alkane | B3LYP-D3/6-311G** |  |  | B3LYP-D4/6-311G** |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ∆H298bind, kJ/mol | ∆S298bind, J/(mol·K) | ∆G298bind, kJ/mol | ∆H298bind, kJ/mol | ∆S298bind, J/(mol·K) | ∆G298bind, kJ/mol |
| B12N12H12 |  |  |  | C24H12 |  |  |
| C2H6 | -16.01 | -151.01 | 28.99 | -17.70 | -156.63 | 28.98 |
| C3H16 | -20.98 | -149.69 | 23.62 | -23.18 | -157.02 | 23.61 |
| C4H10 | -27.25 | -163.72 | 21.54 | -29.67 | -168.70 | 20.60 |

Table S4. Thermodynamic parameters of alkane dimerization within PM6-DH2 method

| Alkane | Parameters of dimerization |  |  | Parameters of dimerization |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ∆H298dim, kJ/mol | S298dim, J/(mol·K) | ΔG298dim, kJ/mol | ∆H298dim, kJ/mol | S298dim, J/(mol·K) | ΔG298dim, kJ/mol |
| For monolayer of the “straight” structure |  |  |  |  |  |  |
| Dimer p |  |  |  | Dimer q |  |  |
| C6H14 | -12.41 | -124.19 | 24.60 | -6.22 | -74.07 | 15.85 |
| C7H16 | -14.81 | -105.36 | 16.59 | -6.23 | -66.15 | 13.49 |
| C8H18 | -17.42 | -114.82 | 16.79 | -6.23 | -65.54 | 13.31 |
| C9H20 | -19.63 | -121.44 | 16.56 | -6.23 | -87.92 | 19.97 |
| C10H22 | -22.29 | -163.37 | 26.39 | -6.22 | -65.93 | 13.43 |
| C11H24 | -24.46 | -133.08 | 15.20 | -6.24 | -64.53 | 12.99 |
| C12H26 | -27.16 | -162.94 | 21.39 | -6.24 | -90.50 | 20.73 |
| C13H28 | -29.59 | -164.13 | 19.32 | -6.24 | -93.13 | 21.51 |
| C14H30 | -32.04 | -164.12 | 16.87 | -6.26 | -74.93 | 16.07 |
| For monolayer of the “herringbone” structure |  |  |  |  |  |  |
| Dimer p |  |  |  | Dimer q |  |  |
| C6H14 | -11.09 | -83.15 | 13.69 | -3.76 | -68.68 | 16.71 |
| C7H16 | -7.10 | -100.23 | 22.77 | - | - | - |
| C8H18 | -10.28 | -115.92 | 24.27 | - | - | - |
| C9H20 | -11.90 | -105.76 | 19.61 | - | - | - |
| C10H22 | -15.07 | -123.36 | 21.69 | - | - | - |
| C11H24 | -22.53 | -127.48 | 15.46 | -3.90 | -64.01 | 15.17 |
| C12H26 | -24.25 | -150.98 | 20.74 | -3.64 | -71.77 | 17.75 |
| C13H28 | -27.39 | -160.24 | 20.36 | -3.59 | -75.87 | 19.01 |
| C14H30 | -30.54 | -161.58 | 17.61 | -3.64 | -67.33 | 16.43 |

Dashes are in the case when the geometrical structure of the dimer does not correspond to the optimized structure of the rest dimers series

Table S5. Thermodynamic parameters of alkane dimerization within PM6-D3H4 method

| Alkane | Parameters of dimerization |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | ∆H298dim, kJ/mol | S298dim, J/(mol·K) | ΔG298dim, kJ/mol | ∆H298dim, kJ/mol | S298dim, J/(mol·K) | ΔG298dim, kJ/mol |
| For monolayer of the “straight” structure |  |  |  |  |  |  |
| Dimer p |  |  |  | Dimer q |  |  |
| C6H14 | -15.65 | -110.35 | 17.24 | -1.67 | -58.32 | 15.71 |
| C7H16 | -18.67 | -122.67 | 17.89 | -2.64 | -69.78 | 18.16 |
| C8H18 | -21.73 | -127.45 | 16.25 | -2.64 | -59.18 | 14.99 |
| C9H20 | -24.76 | -145.17 | 18.50 | -1.57 | -51.90 | 13.90 |
| C10H22 | -27.81 | -151.88 | 17.45 | -1.46 | -54.54 | 14.79 |
| C11H24 | -30.84 | -158.71 | 16.45 | -1.57 | -53.61 | 14.41 |
| C12H26 | -33.90 | -178.15 | 19.19 | -2.31 | -60.70 | 15.77 |
| C13H28 | -36.93 | -188.86 | 19.35 | -1.34 | -50.89 | 13.82 |
| C14H30 | -39.97 | -198.57 | 19.20 | -1.92 | -79.47 | 21.76 |
| For monolayer of the “herringbone” structure |  |  |  |  |  |  |
| Dimer p |  |  |  | Dimer q |  |  |
| C6H14 | -14.02 | -108.92 | 18.44 | -4.40 | -61.74 | 14.00 |
| C7H16 | -15.87 | -103.60 | 15.00 | -4.48 | -69.53 | 16.24 |
| C8H18 | -20.00 | -125.18 | 17.30 | -4.65 | -69.72 | 16.13 |
| C9H20 | -21.83 | -124.89 | 15.38 | -4.60 | -66.76 | 15.30 |
| C10H22 | -26.23 | -148.66 | 18.07 | -4.64 | -74.61 | 17.59 |
| C11H24 | -28.07 | -160.17 | 19.66 | -4.59 | -82.85 | 20.10 |
| C12H26 | -32.32 | -174.26 | 19.61 | -4.53 | -71.02 | 16.64 |
| C13H28 | -34.15 | -178.19 | 18.95 | -4.52 | -79.69 | 19.23 |
| C14H30 | -38.39 | -195.64 | 19.91 | -4.45 | -77.81 | 18.74 |

p-direction

p-direction

q-direction

Dimer p

Dimer q

q-direction

Dimer p

Dimer q

(a)								(b)

Figure S1. Fragment of 2D monolayer structure of alkanes on graphene with the “straight” (a) and “herringbone” (b) molecular packing (by the example of hexane – C150H30 complex)

Table S6. Melting temperature for alkane 2D monolayer on isoelectronic surfaces and 3D bulk phase

| Alkane CnH2n+2 | Melting temperature for alkane 2D monolayer on BNNS surface* |  |  | Melting temperature for alkane 2D monolayer on graphene-like surface* |  |  | Experimental bulk melting point [8] |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Calc. in PM6-D3H4 | Calc. in PM6-D3H4 with correction | Exptl. [7] | Calc. in PM6-DH2 | Calc. in PM6-DH2 with correction | Exptl. [7] |  |
| C6H14 | 222.6 (223.6) | 186.0 | 184.0 | 223.4 (227.1) | 194.0 | 187.8 | 178.0 |
| C7H16 | 237.0 (237.4) | 205.3 | 196.2 | 238.4 (241.7) | 213.8 | 206.8 | 182.6 |
| C8H18 | 249.2 (249.1) | 222.4 | 227.4 | 251.6 (254.2) | 231.8 | 238.9 | 216.3 |
| C9H20 | 259.8 (259.2) | 237.8 | 239.7 | 263.3 (265.0) | 248.2 | 251.3 | 219.5 |
| C10H22 | 269.1 (268.0) | 251.9 | 256.4 | 273.7 (274.5) | 263.4 | 268.3 | 243.3 |
| C11H24 | 277.2 (275.7) | 264.8 | 267.6 | 283.1 (282.8) | 277.6 | 280.7 | 247.4 |
| C12H26 | 284.4 (282.5) | 276.9 | 278.5 | 291.5 (290.2) | 290.8 | 291.1 | 263.5 |
| C13H28 | 290.8 (288.6) | 288.1 | 289.3 | 299.2 (296.7) | 303.3 | 303.4 | 268.0 |
| C14H30 | 296.6 (294.0) | 298.7 | 298.0 | 306.2 (302.7) | 315.1 | 317.4 | 278.7 |
| C15H32 | 301.8 (298.9) | 308.8 | 307.1 | 312.6 (308.0) | 326.3 | 322.6 | 283.0 |
| C16H34 | 306.5 (303.4) | 318.3 | 314.7 | 318.5 (312.9) | 336.9 | 333.0 | 291.0 |

* the values in parentheses correspond to the monolayer of “herringbone” structure

b

a

(a)

a

b

φ

(b)

Figure S2. Illustration of geometrical parameters of the unit cell for 2D monolayer structures of alkanes on graphene with the “straight” (a) and “herringbone” (b) molecular packing

References for Supplementary Materials

- Haque, S.; Rahman, M. A.; Islam, M. A. M.; Hossain, A. Computational Insights into the Electronic, Chemical, and Thermodynamic Properties of Borazine and Its Derivatives. Results in Chemistry, 2025, 17, 102634 – 9 p. doi:10.1016/J.RECHEM.2025.102634

- Boese, R.; Maulitz, A. H.; Stellberg, P. Solid-State Borazine: Does it Deserve to be Entitled “Inorganic Benzene”? Chemische Berichte, 1994, 127 (10): 1887–1889. doi:10.1002/cber.19941271011.

- Nelson, Jr. R. D.; Lide, Jr. D. R.; Maryott, A. A. Selected values of electric dipole moments for molecules in the gas phase. American National Bureau of Standards 1967, 10, 49 p.

- Stull, D. R.; Westrum, E. F. Jr.; Sinke, G. C. The Chemical Thermodynamics of Organic Compounds; John Wiley & Sons: New York, 1969.

- Dean, J. Lange’s handbook of chemistry. New York : McGraw-Hill, Inc. 1999, 1291 p.

- Kilday, M. V.; Johnson, W. H.; Prosen, E. J. Heat of Combustion of Borazine. B3N3H6. J. Research of the National Bureau of Standards – A, Physics and Chemistry, 1961, 65A (2), 101-104.

- Arnold, T.; Parker, J. E.; Macdonald, P. Investigation of the Adsorption of Alkanes on Hexagonal Boron Nitride from Their Liquids and Binary Mixtures, J. Phys. Chem. C 2012, 116, 10599-10606. DOI: 10.1021/jp300649a.

- NIST Standard Reference Database Number 69. In NIST Chemistry WebBook ed. by Linstrom, P. J.; Mallard, W. G. NIST: Gaithersburg, MD, 2012. DOI: https://doi.org/10.18434/T4D303