Treating CsPbI3 Perovskite with Pyrrolidinium Iodide to Improve the Performance of Perovskite Solar Cells

Qixian Zhangab, Yi Guoab, Huicong Liua, Weiping Lia, Liqun Zhua, Haining Chen*a

- School of Materials Science and Engineering, Beihang University, China.

- These authors contributed equally

*Corresponding authors: chenhaining@buaa.edu.cn

Supplementary Material

Fig. S1. XPS spectrum of the blank CsPbI3 and 1mg/ ml PyI treated CsPbI3.

Fig. S2 AFM images of the Py-CsPbI3 perovskite films.

Fig. S3 The corresponding Tauc-plots for the blank CsPbI3 and different concentration of PyI treated CsPbI3 films.

Fig. S4. The valence band edges and cutoff regions of UPS spectra.

Fig. S5 (A) UV-vis spectra of Py2CsPb2I7 and (B) corresponding Tauc-plots.

Fig. S6 Reverse and forward scans of J-V curves for the Py-CsPbI3 devices with different PyI concentrations: (A) 0.5 mg/mL, (B) 1 mg/mL, (C) 2 mg/mL and (D) 3 mg/mL.

Fig. S7 The transient photovoltage decay (TPV) curves of CsPbI3 and Py-CsPbI3 devices.

Table S1. Data related to energy level information of CsPbI3 and Py-CsPbI3 films.

| Type | Ecutoff (eV) | Eonset (eV) | EVBM (eV) | ECBM (eV) | Eg (eV) |
| --- | --- | --- | --- | --- | --- |
| CsPbI3 | 16.42 | 0.86 | -5.66 | -3.98 | 1.68 |
| Py2CsPb2I7 | 16.44 | 1.38 | -6.16 | -3.09 | 3.07 |