The paraffin crystallization in emulsified waxy crude oil by dissipative particle dynamics

Appendix A

A1-Forcefield Parameter

The 12-6 Lennard-Jones (L-J) and DPD interaction potential function is selected to express, and the specific expression is as follows:

(6)

Whereandare the energy and length constants respectively; rij is the distance between the two i, j beads.

Table 1： Conservative force field parameter between beads (DPD units) [1, 2]

| Bead i | Bead j | Type | Interaction Parameter aij() | Cutoff Radius |
| --- | --- | --- | --- | --- |
| [CH3-CH2-CH2] | [CH2-CH2] | DPD | 25.0 | 1.0740 |
| [CH2-CH2] | [CH2-CH2] | DPD | 15.7 | 0.9701 |
| [CH3-CH2-CH2] | [CH3-CH2-CH2] | DPD | 25.0 | 1.0740 |
| [Cu] | [CH3-CH2-CH2] | LJ-12-6 | 5.132 | 0.395 |
| [Cu] | [CH2-CH2] | LJ-12-6 | 5.132 | 0.395 |
| [Cu] | [Cu] | LJ-12-6 | 35.32 | 0.395 |
| [H2O] | [H2O] | DPD | 25.0 | 1.000 |
| [H2O] | [CH2-CH2] | DPD | 45.0 | 1.0370 |
| [H2O] | [CH3-CH2-CH2] | DPD | 45.0 | 1.0370 |
| [Cu] | [H2O] | DPD | 2.032 | 0.245 |

The Bond and Angle interactions shown in the following Table2 and Table 3:

| Table 2： Bond interaction parameter[1, 2] |  |  |  |
| --- | --- | --- | --- |
| Bead i | Bead j |  |  |
| [CH2-CH2-CH3] | [CH2-CH2] | 2500 | 0.45 |
| [CH2-CH2] | [CH2-CH2] | 2500 | 0.35 |

Table 3: Angle interaction parameter[1, 2]

| Bead i | Bead j | Bead k |  |  |
| --- | --- | --- | --- | --- |
| [CH2CH2] | [CH2CH2] | [CH2CH2] | 70 | 180 |
| [CH3-CH2-CH2] | [CH2CH2] | [CH2CH2] | 150 | 169 |

The unit used in DPD is a dimensionless unit that can be converted to and from the real unit. The conversion criteria between the two are as follows, which was placed in the attachment:

Table 4: Dimensionless transformation factor of DPD

| Real units | Dimensionless conversion factor |
| --- | --- |
| Cut-off radius rc (Å) | r=r*rc |
| Energy E (kJ/mol) | E=E*(KBT) |
| Time t (ps) | t=t* |
| Temperature T (K) | T=T*T0 |
| Mass m (g) | M=m*(2mH2O) |
| Pressure p (MPa) |  |

A2-Forcefield Verification

The force field parameters used in this paper are based on the literature of Bray et al. and also combined with our previous work that has validated the force field parameters[1, 2], which has validated the accuracy of force field parameters.

[1] Bray DJ, Anderson RL, Warren PB, Lewtas K. Wax Formation in Linear and Branched Alkanes with Dissipative Particle Dynamics. Journal of Chemical Theory and Computation. 2020;16(11):7109-22.

[2] Li QB, Cao JC, Liu Y, Cheng QL, Liu C. Effect of dispersed water on the paraffin crystallization and deposition of emulsified waxy crude oil via dissipative particle dynamics. Journal of Molecular Liquids. 2021;343.