1 Model Formulation

For building the model, data was divided into training set (80%), validation set (10%) and testing set (10%). Testing set was separated at the very beginning so that it would be remain unseen and get the unbiased prediction at the end to evaluate the robustness the model. Model initially learns from the training set and then it is subjected to the validation set to perform prediction. This step was repeated 10-fold times to get the stable accuracy over the domain and to avoid landing up in bias predictions as the database was small. Then the overall accuracy was quantified by averaging out the MAE values of all 10 prediction and it will be used as criterion for model evaluation and comparison in subsequent steps. Model 1 was optimized by tuning its six important hyper parameters using real-coded genetic algorithm. GA used total population of 60 and maximum iteration of 130 with appropriate crossover, mutation, and elitism values. Model 2 was developed as a stacking model which can best merge the well performing models (Artificial Neural Network (ANN), Random Forest, Catboost and Xgboost) for overall accuracy both locally and globally. Here ANN uses 3 hidden layers with 10 nodes architecture along with non-linear rectifier (ReLU) activation function and Adam optimization technique.

ReLU Function: fx=0,x                                                                  (1)

where x is an input value.

Catboost used GA optimized parameters, Random Forest used grid optimized parameters and Xgboost used default ones. All these four models were then trained and predicted on the test data to generates metadata. Then support vector machine was incorporated as meta model to perform final predictions on the test set using meta data. To evaluate model prediction capability following three statistical methods are used:

Root Mean Square Error (RMSE)=  i=1nyi-yi2n                                 	  (2)

Mean Absolute Error (MAE)=  i=1nyi-yin                                  (3)

Coefficient of Determination  R2=1-i=1nyi-yi2i=1nyi-y2                                        (4)

where yi = original (experimental) value, yi = predicted Value, y= averaged value of the dataset

As discussed before, Model 1 was built to correlate the composition of copper alloys with corresponding properties. To demonstrate its efficacy some of the predictions made by the model are presented and compared in Table 3 and remaining are shown below in Table S1.

Table S1: Accuracies for various ‘Composition to Property’ models

| Machine Learning Models | UTS (MAE (R2 value)) | EC (MAE (R2 value)) |
| --- | --- | --- |
| Support vector regressor | 71.0 (0.58) | 5.98 (0.80) |
| Decision trees regressor | 46.48 (0.72) | 5.82 (0.73) |
| Random forest regressor | 48.66 (0.78) | 4.18 (0.89) |
| XGboost regressor | 46.85 (0.77) | 4.56 (0.86) |
| LightGBM regressor | 53.3 (0.72) | 5.78 (0.80) |
| Histogram gradient boosting regressor | 51.66 (0.73) | 5.46 (0.81) |
| Gradient boosting regressor | 55.55 (0.74) | 4.92 (0.87) |
| ANN | 59.75 (0.8) | 4.82 (0.84) |

Table S2: Comparison of predicted properties of copper alloys with experimental results

| Composition | Electrical conductivity |  |  |  | Ultimate tensile strength |  |  | References |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Experimental result | Model prediction | %Error |  | Experimental result | Model prediction | %Error |  |
| Cu-4.5Cr-3Ag | 47 | 52.2 | 11.06 |  | 818 | 714.3 | 12.67 | [1] |
| Cu-2.6 ZrB2 | 65.4 | 69.8 | 6.73 |  | 395 | 434.7 | 10.05 | [2] |
| Cu-0.01Cr-0.07Zn-2.1Fe-0.02P-0.2 RE-0.2Porosity | 70 | 69.9 | 0.14 |  | 518 | 507.8 | 1.96 | [3] |
| Cu-0.5Cr-0.15Zr | 87 | 86.9 | 0.11 |  | 530 | 530.0 | 0 | [4] |
| Cu-0.18Zr-2.11Ni-0.53Si | 40 | 47.6 | 19.00 |  | 665 | 634.4 | 4.60 | [5] |
| Cu-0.34Cr-0.3Zr | 84 | 84.0 | 0.00 |  | 460 | 461.1 | 0.23 | [6] |
| Cu-0.8Cr-0.15Zr-0.04Mg | 85 | 80.0 | 5.88 |  | 500 | 580.0 | 16 | [7] |
| Cu-3.2Ni-0.7Si | 55 | 45.2 | 17.81 |  | 585 | 695.5 | 18.88 | [8] |
| Cu-5TiB2-4.8Porosity | 65 | 64.9 | 0.15 |  | 371 | 376.8 | 1.56 | [9] |
| Cu-1.5Ni-0.18Si-0.5Zn-0.1P | 47 | 47.2 | 0.42 |  | 685 | 599.4 | 12.49 | [10] |
| Cu-0.3Cr-0.1Zr-0.05Mg | 82 | 82.0 | 0.00 |  | 570 | 590.0 | 3.50 | [11] |
| Cu-0.3Cr-0.2Zn-0.025Sn | 80 | 80.0 | 0.00 |  | 540 | 534.2 | 1.07 | [12] |
| Cu-0.165Fe-0.0350P | 85 | 88.1 | 3.65 |  | 400 | 416.1 | 4.02 | [13] |
| Cu-0.7Cr-0.3Fe | 66 | 73.4 | 11.21 |  | 537 | 415.0 | 22.71 | [14] |
| Cu-0.2Cr-0.1Zr-0.2Zn | 80 | 80.5 | 0.62 |  | 580 | 530.3 | 8.56 | [15] |
| Cu-4Ni-1Si | 48 | 48.0 | 0 |  | 704 | 703.8 | 0.03 | [16] |
| Cu-2.4Ni-0.4Si | 39 | 43.8 | 12.30 |  | 627 | 640.9 | 2.21 | [17] |
| Cu-0.38Cr-0.25Zr-0.07Mg-0.02RE | 83.4 | 83.6 | 0.24 |  | 580 | 573.0 | 1.20 | [18] |
| Cu-0.1Fe-0.03P | 92 | 87.1 | 5.32 |  | 383 | 425.3 | 11.04 | [19] |
| Cu-2.5Ni-0.5Si-0.3Zn | 40 | 40.0 | 0.00 |  | 780 | 780.0 | 0.00 | [10] |
| Cu-0.55Cr-0.25Zr | 82.4 | 84.7 | 2.79 |  | 640 | 501.5 | 21.64 | [20] |
| Cu-0.03Mg-0.6Ni-0.1Si-0.02P | 60 | 69.8 | 16.33 |  | 390 | 503.9 | 29.20 | [21] |
| Cu-0.1Fe-0.03P | 85 | 87.1 | 2.47 |  | 490 | 425.3 | 13.20 | [22] |
| Cu-0.3Cr-2Ni-0.5Si | 49.7 | 48.0 | 3.42 |  | 700 | 699.1 | 0.13 | [23] |
| Cu-0.15Zr-2Ni-0.5Si | 47.5 | 47.5 | 0.00 |  | 587 | 587.7 | 0.12 | [23] |
| Cu-0.6Cr-0.1Zr-0.03Mg | 85 | 84.6 | 0.47 |  | 586 | 585.8 | 0.03 | [18] |
| Cu-3.2Ni-0.75Si-0.3RE | 59.5 | 61.0 | 2.52 |  | 646 | 540.5 | 16.33 | [24] |
| Cu-4.5Cr-3Ag | 47 | 52.2 | 11.06 |  | 818 | 714.3 | 12.67 | [1] |

Table S3: Elementwise Accuracies of 'Property to Composition' Predictive Models in Various Alloying Systems

| Alloy Systems | Alloying Constituents | Machine Learning Models |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Catboost (MAE (R2 value)) | XGboost (MAE (R2 value)) | Random Forest (MAE (R2 value)) |  |
| Cu-Cr-Zr | Cr | 0.02 (0.99) | 0.05 (0.93) | 0.02 (0.99) |  |
|  | Zr | 0.08 (0.82) | 0.1 (0.79) | 0.08 (0.83) |  |
| Cu-Ni-Si | Ni | 0.38 (0.96) | 0.63 (0.90) | 0.38 (0.96) |  |
|  | Si | 0.07 (0.97) | 0.12 (0.93) | 0.07 (0.97) |  |
| Cu-Fe-P | Fe | 0.16 (0.90) | 0.63 (0.90) | 0.16 (0.90) |  |
|  | P | 0.005 (0.98) | 0.12 (0.93) | 0.005 (0.98) |  |
| Cu-Zr-Ni-Si | Zr | 0.11 (0.77) | 0.17 (0.45) | 0.08 (0.84) |  |
|  | Ni | 0.44 (0.93) | 0.84 (0.77) | 0.29 (0.97) |  |
|  | Si | 0.11 (0.93) | 0.20 (0.78) | 0.07 (0.97) |  |
| Cu-Cr-Ni-Si | Cr | 0.08 (0.82) | 0.15 (0.54) | 0.02 (0.99) |  |
|  | Ni | 0.62 (0.90) | 1.13 (0.69) | 0.37 (0.96) |  |
|  | Si | 0.15 (0.89) | 0.26 (0.66) | 0.07 (0.97) |  |
| Cu-Cr-Ni-Si-P | Cr | 0.14 (0.58) | - | 0.02 (0.99) |  |
|  | Ni | 1.04 (0.72) | - | 0.36 (0.96) |  |
|  | Si | 0.30 (0.57) | - | 0.07 (0.97) |  |
|  | P | 0.02 (0.52) | - | 0.004(0.98) |  |  |
| Cu-ZrB2 | ZrB2 | 014 (0.94) | 0.14 (0.94) | 0.14 (0.94) |  |
| Cu-Zr | Zr | 0.09 (0.80) | 0.09 (0.80) | 0.09 (0.80) |  |
| Cu-Ni-Si-P | Ni | 0.49 (0.92) | 0.99 (0.71) | 0.30 (0.97) |  |
|  | Si | 0.12 (0.92) | 0.24 (0.70) | 0.07 (0.97) |  |
|  | P | 0.012 (0.84) | 0.02 (0.51) | 0.005 (0.98) |  |

References

[1]	S. Bera, S. Ghosh Chowdhury, W. Lojkowsky and I. Manna, “Synthesis of CuCr and CuCrAg alloys with extended solid solubility with nano-Al2O3 dispersion by mechanical alloying and consolidation by high pressure sintering”, Materials Science and Engineering A, vol. 558, pp. 298–308, 2012.

[2]	X. Fan, X. Huang, Q. Liu, H. Ding, H. Wang and C. Hao, “The microstructures and properties of in-situ ZrB2 reinforced Cu matrix composites”, Results in Physics, vol. 14, p. 102494, 2019.

[3]	C. Yang, C. Xiang, K. Aaron, X. Cao, C. Longing and Y. Tang, “High temperature copper alloy for lead frame and its making process”, CN1932056, 2009.

[4]	C. Watanabe, R. Monzen and K. Tazaki, “Mechanical properties of Cu-Cr system alloys with and without Zr and Ag”, Journal of materials science, vol. 43, pp. 813–819, 2008.

[5]	X.P. Xiao, B.Q. Xiong, Q.S. Wang, G.L. Xie, L.J. Peng and G.X. Huang, “Microstructure and properties of Cu-Ni-Si-Zr alloy after thermomechanical treatments”, Rare Metals, vol. 32, pp. 144–149 2013.

[6]	L. Peng, “Study on microstructure evolution of Cu-Cr-Zr system alloys and interaction mechanism between alloying elements”, General Research Institute for Nonferrous Metals, 2014.

[7]	X. Zhan, “Thermo-dynamic Calculation and Experimental Research on Non-Vacuum Melting of Cu-Cr-Zr Alloy”, Jiangxi University of Science and Technology, 2009.

[8]	L. Wang, Y. Sun, X. Fu, “Microstructure and properties of Cu-Ni-Si based alloys for lead frame, Journal of Southeast University”, Natural Science Edition, vol. 35, pp. 729–732, 2005.

[9]	D.H. Kwon, K.X. Huynh, T.D. Nguyen, P.P. Choi, M.-G. Chang, Y.J. Yum, J.S. Kim and Y.S. Kwon, “Mechanical Behavior of TiB2 Nanoparticles Reinforced Cu Matrix Composites Synthesized by In-Situ Processing”, Materials Science Forum, vol. 510, pp 346–349, 2006.

[10]	Y. Zhang, M. Lu, Y. Hu, “Development and Study of Cu-Ni-Si Alloy for Lead Frame”, Shanghai Nonferrous Metals, vol. 04, pp. 177–182, 2014.

[11]	Q. Yongqiang, “Design, Preparation and Properties of High Strength and High Conductivity Cu-Cr-Zr Alloy”, Hefie Unversity of Technology, 2013.

[12]	X. Zhang, “Study on Preparation Technology and Properties of Cu-Ni-Si Alloy for Lead Frame”, 2013.

[13]	W. Zhu, G. Yao, Z. Li, H. Zhang, M. Zhao, J. Xia, Y. Zhou and J. Li, “Integrated circuit lead frame copper strip and preparation method thereof”, CN101299424A, 2008.

[14]	H. Fernee, J. Nairn and A. Atrens, “Cold worked Cu-Fe-Cr alloys”, Journal of materials science, vol. 36, pp. 5497–5510, 2001.

[15]	Y. Tomioka and J. Miyake, “A copper alloy development for leadframe”, Proceedings of 1995 Japan International Electronic Manufacturing Technology Symposium, pp. 433–436, IEEE, 1995.

[16]	D. Li, Q. Wang, B. Jiang, X. Li, W. Zhou, C. Dong, H. Wang and Q. Chen, “Minor-alloyed Cu-Ni-Si alloys with high hardness and electric conductivity designed by a cluster formula approach”, Progress in Natural Science: Materials International, vol. 27, no. 4, 467–473, 2017.

[17]	J. Wang, “Study on microstructure and properties of Cu-Ni-Si-Mg alloy used for lead frame”, 2012.

[18]	S. Mu, “New Technology and Theoretical Study on the Preparation of High Strength and High Conductivity Cu-Cr-Zr Alloys”, Central South University, 2008.

[19]	Y. Lin, “Low Alloy Tin Bronze for High Performance Connectors”, Electromechanical Components, vol. 21, pp. 24–27, 2001.

[20]	H. Guojie, X. Xiangpeng, X. Shuisheng, C. Lei, M. Xujun, F. Yao and X. Baiqing, “CuCrZr alloy with high strength and high conductivity, and preparation and processing method thereof”, CN102534291A, 2012.

[21]	G.K. Young and Y.H. In, “Copper alloys for electrical and electronic parts”, US5334346A, 1994.

[22]	P. Liu, D. Zhan and B. Tian, “High Performance Copper Alloy and its Processing Technology”, 2005.

[23]	W. Wang, H. Kang, Z. Chen, Z. Chen, C. Zou, R. Li, G. Yin and T. Wang, “Effects of Cr and Zr additions on microstructure and properties of Cu-Ni-Si alloys”, Materials Science and Engineering A, vol. 673, pp. 378–390, 2016.

[24]	W. Zhong, P. Liu, Kangbusi, S. Wang, Q. Dong, X. Li, B. Tian, D. Zhao, L. Golden, W. Cheng, H. Li and G. Huang, “ISIC leading wire frame copper tape and its production process”, CN1477220A, 2008.